## Slide 1
EDX)
ABSTRACT
EXPERIMENTS
Pd-Au nano-sized alloy catalysts supported on TiO2 submicron-sized fibers have been developed by electrospinning, calcination of the polymer template fibers, and hydrazine reduction. The morphologies, crystal structure, and textural properties (surface area, pore size, and volume) of Pd-Au/TiO2 fibers materials were evaluated with electron microscopy (SEM, TEM, and HRTEM), X-ray Diffraction(XRD), and BET nitrogen adsoprtion. For the alloy effect induced by the Pd-Au formation, the ensemble (geometric) effect and ligand effect (charge transfer) in Pd-Au nanoparticles were investigated with X-ray photoelectron spectroscopy (XPS) and Fourier transform infrared spectroscopy (FTIR) to understand the formation of alloyed Pd-Au particles of different metal composition with consequent modification of their electronic and geometric properties.
The catalytic activity of these materials were tested in carbon monoxide oxidation reaction using a plug-flow reactor. The results showed that the performance was optimal for a catalyst of composition Pd2Au1 molar ratio that was active at 125°C, which had higher dispersion of active components and better catalytic performance compared to monometallic particle Au/TiO2 and Pd/TiO2 fiber media. Moreover, the improved reaction activity of Pd2Au1/TiO2 fiber medium was attributed to a decreased in the activation energy.
RESULTS AND DISCUSSION
Figure 1.
Overall preparation procedures
of 2.3cm fibrous fiber media based on catalytic nanoparticles (Au, Pd, or
Pd-Au) doped TiO2 submicron sized
fiber.
Step (A) : electrospinning solutions,
Step (B) : electrospinning, calcination,
and reduction of only Au, Pd, or
Pd-Au/TiO2
Step(C) : catalytic media out of
Catalytic submicron sized TiO2 fibers
and Al2O3 microfibers [(1) Au/TiO2,
(2) Pd1Au2/TiO2, (3) Pd1Au1/TiO2,
(4) Pd2Au1/TiO2, and (5) Pd/TiO2]
- Microscope Study (SEM, TEM)
- X-Ray Diffraction Study (XRD)
Carbon Monoxide over Pd-Au Alloy Nanoparticle doped Fibrous TiO2 Fiber Media
Hyeon Ung Shin, Dinesh Lolla, Ahmed Abutaleb, and George G. Chase
RESULTS AND DISCUSSION
- X-ray Photoelectron Spectroscopy (XPS)
Figure 6. XPS peaks of Pd 3d (A) and Au 4f (B) after and before reduction
11
- Transmission Electron Microscope (HRTEM, SAED)
- Catalytic Performance
RESULTS AND DISCUSSION
Material | Fiber size (nm) | Particle size (nm) | Paticle composition | Metal loading(wt %)
Au/TiO2 | 119±53 | 19.8±1.9 | Au | 5.3
Pd1Au2/TiO2 | 124±57 | 14.2±1.7 | Pd35Au65 | 4.9
Pd1Au1/TiO2 | 107±51 | 9.3±1.1 | Pd52Au48 | 4.7
Pd2Au1/TiO2 | 99±49 | 7.2±0.8 | Pd68Au32 | 5.0
Pd/TiO2 | 105±55 | 8.5±0.6 | Pd | 4.8
Table 1.Fiber size, particle size, composition and metal loading
Figure 3. SEM (left column, Top right inset : Fiber size distribution) TEM (right column) images for (A) Au/TiO2, (B) Pd1Au2/TiO2, (C) Pd1Au1/TiO2, (D) Pd2Au1/TiO2, and (E) Pd/TiO2
- Energy Dispersive X-Ray Analysis (EDX)
Figure 2. SEM-EDX mapping of Pd2Au1/TiO2 fibers
Figure 4.
X-ray
diffraction
peaks of Au/TiO2, Pd-Au/TiO2, Pd/TiO2
Material | SSAa (m2/g) | Pore diameterb (nm) | Pore widthc (nm) | Pore volumed (cm3/g)
Au/TiO2 | 55.5 | 5.5 | 6.1 | 0.085
Pd1Au2/TiO2 Pd1Au1/TiO2 | 72.5 87.6 | 4.3 5.3 | 4.5 6.1 | 0.078 0.134
Pd2Au1/TiO2 Pd/TiO2 | 103.3 115.2 | 4.8 4.9 | 5.2 5.5 | 0.132 0.156
aBET specific surface area, bBJH adsorption average pore diameter, cadsorption average pore width, dBJH adsorption cumulative volume of pores
Table 2. Textural properties of Pd-Au/TiO2, Au/TiO2, and Pd/TiO2 fibers
Figure 7. HRTEM images of Pd2Au1 particle (A) after calcination in air at 550°C for 4 hours (B) after consequent reduction (inset : FFT pattern
A
B
Figure 8. (A) CO conversion (%) of Pd-Au doped TiO2 fiber media and (B) FT-IR spectra for CO chemisorbed on Au/TiO2, Pd/TiO2, and Pd-Au/TiO2 fiber media
- Brunauer, Emmett, and Teller Surface Area (BET)
Figure 5.
(A) N2 adsorption-desorption isotherms and
(B) BJH pore size distribution curves of Pd-Au/TiO2 nanofibers
Figure 9. (A) Turnover frequency (TOF) and (B) Arrhenius plots for CO oxidation
CONCLUSION
- The Synergetic effect induced by the Pd-Au alloy formation could strongly influence the Pd-Au particle size and catalytic performances.
- The decrease of the particle size achieved by the alloy Pd-Au (Pd2Au1 and Pd1Au1) could avoid the growth of metal particles.